First-Principles Investigation of Structural, Mechanical, Electronic, and Thermal Properties of Half-Heusler ZrPtSn

Lynet Allan*, Julius M. Mwabora, Winfred M. Mulwa, Edwin Mapasha, Robinson J. Musembi

*Corresponding author(s). E-mail(s): allanlynet3@students.uonbi.ac.ke

Supplementary Material

Manuscript Number: MRSA-D-25-00099R1

APPENDICES

Appendix 1: The crystal structure and lattice constants of ZrPtSn half Heusler Alloy

Figure 1;(a) The crystal structure of ZrPtSn half Heusler Alloy, (b) Energy vs Lattice constant without SOC effects, and (c) Energy vs Lattice constant with SOC effects

Appendix 2: Elastic Properties and Stiffness Matrix Eigenvalues of ZrPtSn

Table 1(a)Elastic Properties of ZrPtSn

| Property | Value |
| --- | --- |
| C11 | 180.1 |
| C12 | 26.8 |
| C44 | 71.1 |
| Poisson’s Ratio (ν) | 0.30 |
| Universal Anisotropy (AU) | 0.09 |

Table 1 (b)Stiffness Matrix Eigenvalues of ZrPtSn

| Eigenvalue | λ1 | λ2 | λ3 | λ4 | λ5 | λ6 |
| --- | --- | --- | --- | --- | --- | --- |
| Value (GPa) | 70 | 70 | 70 | 108 | 108 | 402 |

Appendix 3:  Averaged and Variational Elastic Properties of ZrPtSn

Table 2 (a) Averaged Elastic Properties of ZrPtSn

| Averaging Scheme | Bulk Modulus (GPa) | Young's Modulus (GPa) | Shear Modulus (GPa) | Poisson's Ratio |
| --- | --- | --- | --- | --- |
| Voigt (Kv, Ev, Gv, νv) | 134 | 164.74 | 63.6 | 0.2951 |
| Reuss (KR, ER,GR,νR) | 134 | 162.46 | 62.583 | 0.29794 |
| Hill (KH, EH, GH, νH) | 134 | 163.6 | 63.091 | 0.29652 |

### Table 2 (b) Variations of the Elastic Moduli for ZrPtSn

| Property | Emin (GPa) | Emax (GPa) | βmin (TPa⁻¹) | βmax (TPa⁻¹) | Gmin (GPa) | Gmax (GPa) | νmin | νmax |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Value | 142.82 | 178.86 | 2.4876 | 2.4876 | 54 | 70 | 0.20173 | 0.37976 |
| Anisotropy | 1.252 | 1.0000 | 1.296 | 1.8825 | -- | -- | -- | -- |

Appendix 4:  Elastic moduli and anisotropy variations for ZrPtSn, analyzed using ELATE software.

Figure 4 ; The directional dependencies of (a) Young’s modulus, (b) Linear Compressibility, (c) Poisson’s ratio and (d) shear modulus (blue indicates the maximum values while green represents the minimum values across crystallographic directions.).